| Component - Plastics | E52579 |
| --- | --- |
| MITSUI CHEMICALS INC |  |
| SHIODOME CITY CENTER, #1-5-2, HIGASHI-SHINBASHI, MINATO-KU, TOKYO 105-7117 JP |  |
| E430N(#)(r3) |  |
| Polyamide (PA), "ARLEN", furnished as pellets |  |

|  | Min Thk | Flame |  |  | RTI | RTI | RTI |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Color | (mm) | Class | HWI | HAI | Elec | Imp | Str |
| ALL | 0.80 | V-0 | - | - | 110 | 115 | 120 |

| Comparative Tracking Index (CTI): | 1 | Inclined Plane Tracking (IPT): | - |
| --- | --- | --- | --- |
| Dielectric Strength (kV/mm): | - | Volume Resistivity (10x ohm-cm) : | - |
| High-Voltage Arc Tracking Rate (HVTR): | - | High Volt, Low Current Arc Resis (D495): | - |
| Dimensional Stability (%): | - |  |  |

| (#) - | May be followed by 1 to 4 digits and/or letters |
| --- | --- |
| (r3) - | Virgin and regrind up to 50% by weight inclusive have the same flammability properties to the minimum thickness of 0.8 mm only. |

ANSI/UL 94 small-scale test data does not pertain to building materials, furnishings and related contents. ANSI/UL 94 small-scale test data is intended solely for determining the flammability of plastic materials used in the components and parts of end-product devices and appliances, where the acceptability of the combination is determined by UL.

| Report Date:2019-3-20 Last Revised: 2022-3-20 | © 2022UL LLC |  |
| --- | --- | --- |

IEC and ISO Test Methods

|  |  |  | Thickness |  |
| --- | --- | --- | --- | --- |
| Test Name | Test Method | Units | Tested (mm) | Value |
| Flammability | IEC 60695-11-10 | Class (color) | 0.80 | V-0 (ALL) |
| Glow-Wire Flammability (GWFI) | IEC 60695-2-12 | C | - | - |
| Glow-Wire Ignition (GWIT) | IEC 60695-2-13 | C | - | - |
| IEC Comparative Tracking Index | IEC 60112 | Volts (Max) | - | - |
| IEC Ball Pressure | IEC 60695-10-2 | C | - | - |
| ISO Heat Deflection (1.80 MPa) | ISO 75-2 | C | - | - |
| ISO Tensile Strength | ISO 527-2 | MPa | - | - |
| ISO Flexural Strength | ISO 178 | MPa | - | - |
| ISO Tensile Impact | ISO 8256 | kJ/m2 | - | - |
| ISO Izod Impact | ISO 180 | kJ/m2 | - | - |
| ISO Charpy Impact | ISO 179-2 | kJ/m2 | - | - |

2022UL LLC